Task 7.6—Apply Coating Using Spray Applications

1.0	Task Description

This task consists of applying coating to a pipeline facility by spray method.

This task begins with determination of the type of coating to be used. This task ends when all required information is recorded per the operator’s procedure.

The performance of this covered task may require the performance of other covered tasks such as:

Prepare Surface for Coating Using Hand and Power Tools (reference Task 7.2);

Prepare Surface for Coating by Abrasive Water Blasting (reference Task 7.3);

Prepare Surface for Coating by Abrasive Blasting Methods Other Than Water (reference Task 7.4);

Perform Coating Inspection (reference Task 7.7).

This task does not include but may lead to the performance of other covered tasks such as:

Inspect the Condition of External Coating on Buried or Submerged Pipe (reference Task 5.3);

Visual Inspection of Atmospheric Coating (reference Task 7.1).

2.0	Knowledge Component

The purpose of this task is to apply protective coating to pipeline components.

An individual performing this task shall have knowledge of:

a)	methods of applying coating by spraying, including:

1)	high volume/low pressure;

2)	airless spray.

- Methods to determine appropriate weather conditions for coating application.

Terms applicable to this task:

orange peel

The dimpled appearance of a dried coating resembling the surface of a navel orange.

overspray

Dry, flat, pebbly surface resulting from paint particles falling outside spray pattern.

sags

Nonuniform downward flow of a wet-applied coating under the force of gravity that results in an uneven coating having a thick lower edge.

wrinkling

Formation of a surface appearance in a coating resembling the skin of a prune, usually caused by application shortcomings.

Abnormal operating conditions (AOCs) associated with the performance of this task include the following:

| AOC Recognition | AOC Reaction |
| --- | --- |
| Pipeline surface not properly prepared for coating (e.g. contaminated surface). | Stop task activities and make appropriate notifications per the operator’s procedures. |
| Weather conditions change and are no longer suitable for coating application. | Stop task activities and make appropriate notifications per the operator’s procedures. |

3.0	Skill Component

To demonstrate proficiency of this task, an individual shall perform the following steps:

| Step | Action | Explanation |
| --- | --- | --- |
| 1 | Determine what type of coating is applicable to the specified pipeline component. | Check that the coating to be applied is compatible with the existing coating system. |
| 2 | Select and assemble the tools and equipment necessary for application as required by coating specification. | Verify that the proper type of spray equipment is selected per Operator and Manufacturer procedures and specifications. |
| 3 | Ensure that weather conditions are suitable for coating operations. | Temperature of pipeline component and dew point are critical to ensure proper adhesion. |
|  | Ensure surface preparation for coating application and free of all contaminants. | Verify Anchor Profile meets Manufacturer specifications and ensure surface is free of contaminants. |
| 4 | Prepare coating for application. | If applicable, mix coating according to coating specification. Ensure that coating has not exceeded shelf life. |
| 5 | Apply coating per specification. | Verify that coating applied has adequate coverage and thickness. Protect coating, as required, until cured to prevent contamination. |
| 6 | Make appropriate notifications and documentation per the operator’s procedures. | Follow the operator’s policies/procedures for appropriate documentation, notification protocol, and actions required. |