Task 5.1—Examine for Mechanical Damage on Buried or Submerged Pipe

1.0	Task Description

Each time a pipeline is exposed, the operator shall perform an inspection/examination of the pipe and the coating for evidence of damage and/or abnormalities. This task is to verify whether mechanical damage, such as dents, gouges, etc., exist on the pipeline and to ensure that proper documentation and reporting have occurred.

This task begins after the pipeline surface has been prepared for inspection. This task ends after inspection results are documented and reported.

This task does not include but may lead to the performance of other covered tasks such as:

Examine for External Corrosion on Buried or Submerged Pipe (reference Task 5.2);

Inspect the Condition of External Coating on Buried or Submerged Pipe (reference Task 5.3);

Coating tasks (reference Task 7.2, Task 7.3, Task 7.4, Task 7.5, Task 7.6, and Task 7.7);

Measure Pit Depth with Pit Gauge (reference Task 8.1);

Measure Wall Thickness with Ultrasonic Meter (reference Task 8.2);

Measure Corroded Area (reference Task 8.3).

2.0	Knowledge Component

An individual performing this task shall have knowledge of:

- identification of characteristics of mechanical damage and corrosion;

- types of coating and the ways that it can mask mechanical or corrosion damage.

- Proper documentation, which may include weld seams, station markers, GPS coordinates, analog clock face representation, and direction of flow.

Terms applicable to this task:

mechanical damage

Visible physical damage to the metallic surface of the pipeline that, at a minimum, may include one or more of the defects listed below:

—	buckle

A bend, bulge, or kink that can cause flattening or changes in the curvature of the pipe.

—	dent

A depression in the surface that has been created by external forces on the pipeline with no visual evidence of metal loss.

—	gouge

A groove in which metal has been removed or displaced from the surface.

—	scratch

A thin, shallow cut or mark on the surface.

Abnormal operating conditions (AOCs) associated with the performance of this task include the following:

| AOC Recognition | AOC Reaction |
| --- | --- |
| Discovery of damage (e.g. mechanical damage or corrosion) on pipeline facilities or components. | Make appropriate notifications according to the operator’s procedures. Complete other actions, including documentation, as required. |
| Unexpected hazardous product encountered when visually observing pipe for integrity issues. | Stop task activities, eliminate ignition source(s), and notify appropriate personnel. |

3.0	Skill Component

To demonstrate proficiency of this task, an individual shall perform the following steps:

| Step | Action | Explanation |
| --- | --- | --- |
| 1 | Visually observe the exposed pipe for integrity issues, such as evidence of a release or significant metal deformation. | Confirms the pipeline is safe for operation and continued task performance. If the observation identifies integrity issues that are not safe, discontinue the task and make immediate notifications. |
| 2 | Confirm that the pipeline surface has been prepared for the mechanical damage inspection. | Proper surface preparation is critical to identifying and locating all types of mechanical damage present on the exposed pipe. |
| 3 | Inspect the exposed pipeline to determine if mechanical damage exists. | Inspection for mechanical damage is critical to identifying potential risks that need further assessment to avoid future leaks or failures. |
| 4 | Identify the type(s) and location(s) of mechanical damage. | The type(s) and location(s) of the damage are used to determine later actions, such as whether repairs are needed and, if so, what kind of repair is needed. There are a variety of methods to describe the location of the damage. One of the more common methods is to locate the damage circumferentially with respect to a clock face. The location of the seam weld and the longitudinal distance to the nearest girth weld are also typically reported. |
| 5 | Make notifications per the operator’s procedures. | Follow the operator’s policies/procedures for appropriate documentation, notification protocol, and actions required. |