Task 5.2—Examine for External Corrosion on Buried or Submerged Pipe

1.0	Task Description

Each time a pipeline is exposed, the operator shall perform an inspection/examination of the pipe and the coating for evidence of corrosion. The inspection verifies whether external corrosion exists on the pipeline.

This task begins after the pipeline surface has been prepared for inspection. This task ends after inspection results are documented and reported.

This task does not include but may lead to the performance of other covered tasks such as:

Examine for Mechanical Damage on Buried or Submerged Pipe (reference Task 5.1);

Inspect the Condition of External Coating on Buried or Submerged Pipe (reference Task 5.3);

Coating tasks (reference Task 7.2, Task 7.3, Task 7.4, Task 7.5, Task 7.6, and Task 7.7);

Measure Pit Depth with Pit Gauge (reference Task 8.1);

Measure Wall Thickness with Ultrasonic Meter (reference Task 8.2);

Measure Corroded Area (reference Task 8.3).

2.0	Knowledge Component

An individual performing this task shall have knowledge of:

- identify characteristics of mechanical damage and corrosion;

- types of coating and the ways that it can mask mechanical or corrosion damage.

- Proper documentation, which may include weld seams, station markers, GPS coordinates, analog clock face representation, and direction of flow.

Terms applicable to this task:

general corrosion

An electrochemical reaction that takes place uniformly over the surface of steel, thereby causing general thinning of the component that could lead to eventual failure of the material.

localized corrosion

Individual areas of pitting or general corrosion areas at discrete sites that may also contain pitting. Areas of localized corrosion in the area of girth or longitudinal welds should be identified and documented.

pitting

An electrochemical reaction that creates metal loss of the outer surface in small, crater-like depressions that have the potential to cause rapid wall loss.

Abnormal operating conditions (AOCs) associated with the performance of this task include the following:

| AOC Recognition | AOC Reaction |
| --- | --- |
| Discovery of damage (e.g. mechanical damage or corrosion) on pipeline facilities or components. | Make appropriate notifications according to the operator’s procedures. Complete other actions, including documentation, as required. |
| Unexpected hazardous product encountered when visually observing pipe for integrity issues. | Stop task activities, eliminate ignition source(s), and notify appropriate personnel. |

3.0	Skill Component

To demonstrate proficiency of this task, an individual shall perform the following steps:

| Step | Action | Explanation |
| --- | --- | --- |
| 1 | Visually observe the exposed pipe for integrity issues such as evidence of a release or significant metal deformation. | Confirms the pipeline is safe for operation and continued task performance. If the observation identifies integrity issues that are not safe, discontinue the task and make immediate notifications. |
| 2 | Confirm that the pipeline surface has been prepared for the external corrosion inspection. | Proper surface preparation is critical to identifying and locating all types of external corrosion present on the exposed pipe. |
| 3 | Examine the exposed pipe for any areas of external corrosion. | Inspection for external corrosion is critical to identifying potential risks that need further assessment to avoid future leaks or failures. |
| 4 | Identify the type(s) and location(s) of any corrosion on the pipeline. | The type(s) and location(s) of the corrosion are used to determine later actions such as whether repairs are needed and, if so, what kind of repair is needed. There are a variety of methods to describe the location of the corrosion. One of the more common methods is to locate the corrosion circumferentially with respect to an analog clock face. The location of the seam weld and the longitudinal distance to the nearest girth weld are also typically reported. |
| 5 | Make notifications per the operator’s procedures. | Follows the operator’s policies/procedures for appropriate documentation, notification protocol, and actions required. |