Task 5.3—Inspect the Condition of External Coating on Buried or Submerged Pipe

1.0	Task Description

Each time the pipeline is exposed, the operator shall perform an inspection/examination of the pipe and the coating. The inspection should verify whether the coating is intact (free from damage and degradation) and is adequately bonded to the pipe’s surface.

This task begins after the coated pipeline is exposed. This task ends after coating inspection results are documented and reported.

This task does not include but may lead to the performance of other covered tasks such as:

Examine for Mechanical Damage on Buried or Submerged Pipe (reference Task 5.1);

Examine for External Corrosion on Buried or Submerged Pipe (reference Task 5.2);

Coating tasks (reference Task 7.2, Task 7.3, Task 7.4, Task 7.5, Task 7.6, and Task 7.7).

2.0	Knowledge Component

An individual performing this task shall have knowledge of:

- types of coating and how to identify the different types of mechanical or corrosion damage.

- Proper documentation reference points, which may include weld seams, station markers, GPS coordinates, analog clock face representation, and direction of flow.

Terms applicable to this task:

bonding

The joining of the coating system and the pipeline in a manner where they are adhered or united by means of adhesive, heat, or pressure.

coating abnormalities:

coating disbondment

Failure of the bond between the coating and the pipe’s surface.

—	cracking—as it relates to coatings

A physical separation to otherwise bonded coating that has an appearance of fissures.

—	holiday

An undesirable discontinuity or break in the coating system. Electronic testing devices detect flaws in the protective coating.

coating abnormality causes

Change or failure of the coating attributed to one or several of the following:

formulation-related (e.g. checking, cracking, discoloration, and similar phenomena);

improper coating selection;

incompatibility with the surface over which it is applied;

improper or poor surface preparation;

improper application (e.g. inadequate thickness, pinholes, overspray, improper drying, and improper curing);

adhesion-related, structural surface issues (e.g. sharp edges, crevices, skip welds, and back-to-back angles);

exterior forces (e.g. chemical exposure, abrasion, reverse impact, and severe weathering).

pipeline coating types

Pipeline coating types include the following:

asphalt coatings;

coal tar coatings;

extruded coatings;

fusion-bonded epoxy coatings;

petrolatum coating products;

shrink sleeve products;

tape coatings.

Abnormal operating conditions (AOCs) associated with the performance of this task include the following:

| AOC Recognition | AOC Reaction |
| --- | --- |
| Discovery of damage (e.g. mechanical damage or corrosion) on pipeline facilities or components. | Make appropriate notifications according to the operator’s procedures. Complete other actions, including documentation, as required. |
| Unexpected hazardous product encountered when visually observing pipe for integrity issues. | Stop task activities, eliminate ignition source(s), and notify appropriate personnel. |

3.0	Skill Component

To demonstrate proficiency of this task, an individual shall perform the following steps:

| Step | Action | Explanation |
| --- | --- | --- |
| 1 | Visually observe the exposed pipe for major integrity issues, such as evidence of a release or significant metal deformation. | Helps ensure that the pipeline is safe for operation and continued task performance. If the observation identifies integrity issues that are not safe, discontinue the task and make immediate notifications. |
| 2 | Identify the type of existing coating. | It is necessary to be able to identify the type of coating that exists on the pipe so that a proper coating inspection can be conducted. |
| 3 | Examine the exposed coated pipe and determine if there are any flaws or abnormalities in the coating. | Inspection of the coating is critical to identifying potential risks that need further assessment to avoid future leaks or failures. |
| 4 | Identify the type and location of coating damage, if any. | The type and location of the damage are used to determine later actions, such as whether repairs are needed and, if so, what kind of repair is needed. There are a variety of methods to describe the location of the damage. One of the more common methods is to locate the damage circumferentially with respect to an analog clock face. The location of the seam weld and the longitudinal distance to the nearest girth weld are also typically reported. |
| 5 | Make notifications per the operator’s procedures. | Follow the operator’s policies/procedures for appropriate documentation, notification protocol, and actions required. |