Task 7.1—Perform Visual Inspection of Atmospheric Coatings

1.0	Task Description

This task consists of the visual inspection of aboveground pipeline components normally exposed to atmospheric conditions.

This task begins with the identification of the component to be inspected. This task ends when the component has been visually inspected and all required information is documented per operator procedure.

The performance of this covered task may require the performance of other covered tasks such as:

Perform Coating Inspection (reference Task 7.7).

This task does not include but may lead to the performance of other covered tasks such as:

Coating preparation and application tasks (reference Task 7.2, Task 7.3, Task 7.4, Task 7.5, and Task 7.6),

Measure Pit Depth with Pit Gauge (reference Task 8.1);

Measure Wall Thickness with Ultrasonic Meter (reference Task 8.2);

Measure Corroded Area (reference Task 8.3).

2.0	Knowledge Component

The purpose of this task is to visually inspect exposed pipeline components to identify signs of atmospheric corrosion.

An individual performing this task shall have knowledge of:

types of coating and how to identify the different types of mechanical or corrosion damage.

Proper documentation, which may include the line name or system information

Terms applicable to this task:

alligatoring

Pronounced wide cracking over the surface of a coating, which has the appearance of alligator hide.

atmospheric corrosion

Types of rust (spotting, pin point, pitting, perforation, etc.).

blistering

A dome-shaped projection on the surface of a coating resulting from the local loss of adhesion and lifting of the film from an underlying coat or from the base substrate.

blushing

Whitening and loss of gloss of a coating, usually organic, caused by moisture.

chalking

The development of loose, removable powder (pigment) at the surface of an organic coating, usually caused by weathering.

checking

The development of slight breaks in a coating that do not penetrate to the underlying surface.

cracking

Fracture of a material along a path that produces a linear discontinuity (without complete separation).

disbondment

The loss of adhesion between a coating and the substrate.

mechanical damage

physical damage

Damage resulting from abrasion or impacts to the surface of the coated surface.

orange peel

The dimpled appearance of a dried coating resembling the surface of a navel orange.

peeling

Detachment or partial detachment of a coating from the substrate or undercoat.

pinhole

A minute hole through a coat or coats that exposes an underlying coat or the substrate.

sags

Nonuniform downward flow of a wet-applied coating under the force of gravity that results in an uneven coating having a thick lower edge.

soil stress

Typically created by gravel/backfill pressure as it settles around a transitional zone (air-to-soil); the result is often a “bag and sag” in the coating.

wrinkling

Formation of a surface appearance in a coating resembling the skin of a dried prune, usually caused by application shortcomings.

Abnormal operating conditions (AOCs) associated with the performance of this task include the following:

| AOC Recognition | AOC Reaction |
| --- | --- |
| Discovery of damage (e.g. mechanical damage or corrosion) on pipeline facilities or components. | Make appropriate notifications according to the operator’s procedures. Complete other actions, including documentation, as required. |

3.0	Skill Component

To demonstrate proficiency of this task, an individual shall perform the following steps:

| Step | Action | Explanation |
| --- | --- | --- |
| 1 | Confirm the correct location for inspection. | Validates that the correct pipeline component is being inspected. |
| 2 | Identify and confirm type of surface to be evaluated (coating/paint/bare). | This helps determine the equipment and methods to be used for the evaluation. |
| 3 | Perform visual inspection of coating. | Be sure to inspect all required components, including 360 degrees of the pipe. Critical areas of inspection would be: at soil-to-air interfaces; under thermal insulation; under disbonded coatings; at pipe supports; in splash zones; at deck penetrations; in spans over water. |
| 4 | Inspect pipeline components for any atmospheric corrosion. | Identify any areas of rust, spotting, pin point, pitting, or perforation. |
| 5 | Make notifications per the operator’s procedures. | Follow the operator’s policies/procedures for appropriate documentation, notification protocol, and actions required. |