Task 7.2—Prepare Surface for Coating Using Hand and Power Tools

1.0	Task Description

This task consists of preparing the surface for coating using hand and power tools.

The task begins with visually inspecting the surface area to be prepared in order to determine the proper method to use. This task ends when the surface is ready for coating application and all required information is recorded per the operator’s procedure.

The performance of this covered task may require the performance of other covered tasks such as:

Inspect the Condition of External Coating on Buried or Submerged Pipe (reference Task 5.3);

Visual Inspection of Atmospheric Coating (reference Task 7.1);

Perform Coating Inspection (reference Task 7.7).

This task does not include but may lead to the performance of other covered tasks such as:

- Apply Coating Using Hand Application Methods (reference Task 7.5);

- Apply Coating Using Spray Applications (reference Task 7.6).

2.0	Knowledge Component

The purpose of this task is to prepare surface for coating.

An individual performing this task shall have knowledge of:

- surface conditions and which type of tool is needed for surface preparation;

- coating removal, cleaning, and preparation of pipe to accept coating repair;

- coating manufacturer’s specifications for application or repairs to the coating.

Terms applicable to this task:

hand power tool cleaning

The removal of any loose rust, loose mill scale, and loose paint to a degree specified by using a chipping power tool, a power sander, or a wire wheel, etc.

hand tool cleaning

The removal of any loose mill scale, loose rust, and loose paint to a degree specified by hand chipping, scraping, or sanding. Hand cleaning tools include wire brushes, files, scrapers, knives, chisels, chipping hammers, rags, etc.

hand wash

The removal of oil, dirt, soil, grease, and other contaminants by hand with solvent and/or detergents, etc.

Abnormal operating conditions (AOCs) associated with the performance of this task include the following:

| AOC Recognition | AOC Reaction |
| --- | --- |
| Discovery of damage (e.g. mechanical damage or corrosion) on pipeline facilities or components. | Make appropriate notifications according to the operator’s procedures. Complete other actions, including documentation, as required. |
| Unexpected hazardous product encountered when preparing surfaces for coating. | Stop task activities, eliminate ignition source(s), and notify appropriate personnel. |

3.0	Skill Component

To demonstrate proficiency of this task, an individual shall perform the following steps:

| Step | Action | Explanation |
| --- | --- | --- |
| 1 | Visually inspect the surface area to be prepared to determine the proper method to use. | This is necessary to determine if hand tool cleaning, power tool cleaning, and/or hand washing is required. It also determines the proper steps and tools for cleaning and surface preparation. |
| 2 | Remove contaminants from specified area, if present. | This is necessary to avoid grease or oil causing contamination of tools and surface. NOTE Utilize appropriate personal protective equipment to protect from contact or injuries from solvents/detergents, dust, projectiles, and hand/power tools. |
| 3 | Remove existing coating, if present. | Address hazardous coatings (e.g. containing asbestos or lead) in accordance with regulatory requirements and operator procedures. NOTE If coating to be applied meets existing coating, the transition may be made by feathering the existing coating at the interface. |
| 4 | Verify that surface preparation meets operator standards or specifications. | — |
| 5 | Make notifications per the operator’s procedures. | Follow the operator’s policies/procedures for appropriate documentation, notification protocol, and actions required. |