Task 7.3—Prepare Surface for Coating by Abrasive Water Blasting

1.0	Task Description

This task consists of preparing the surface by different types of abrasive water blasting.

The task begins with identification of the area to be blasted. This task ends when the surface is ready for coating application and all required information has been documented per the operator’s procedure.

The performance of this covered task may require the performance of other covered tasks such as:

Inspect the Condition of External Coating on Buried or Submerged Pipe (reference Task 5.3);

Visual Inspection of Atmospheric Coating (reference Task 7.1);

Perform Coating Inspection (reference Task 7.7).

This task does not include but may lead to the performance of other covered tasks such as:

- Apply Coating Using Hand Application Methods (reference Task 7.5);

- Apply Coating Using Spray Applications (reference Task 7.6).

2.0	Knowledge Component

The purpose of this task is to prepare surface for coating.

An individual performing this task shall have knowledge of:

- equipment setup logistics and possible environmental concerns;

- coating removal, cleaning, and preparation of pipe to accept coating repair;

- hazards related to high-pressure discharge;

- coating manufacturer’s specifications for application or repairs to the coating;

- surface preparation standards for water blast cleaning.

Three types of abrasive water blasting, including the following:

- grit blast with shroud—grit is emitted in center of a water shroud;

- sand injected water blast—sand or other medium is blended in water stream at nozzle;

- slurry blast—water and grit mixed together in constantly agitated reservoir.

Terms applicable to this task:

This section intentionally left blank.

Abnormal operating conditions (AOCs) associated with the performance of this task include the following:

| AOC Recognition | AOC Reaction |
| --- | --- |
| Discovery of damage (e.g. mechanical damage or corrosion) on pipeline facilities or components. | Make appropriate notifications according to the operator’s procedures. Complete other actions, including documentation, as required. |
| Unexpected hazardous product encountered when preparing surfaces for coating. | Stop task activities, eliminate ignition source(s), and notify appropriate personnel. |

3.0	Skill Component

To demonstrate proficiency of this task, an individual shall perform the following steps:

| Step | Action | Explanation |
| --- | --- | --- |
| 1 | Identify area to be abrasive water blasted. | This is necessary to determine where to set up equipment. |
| 2 | Set up equipment logistically per job requirements. | Confirms safe and efficient operations. |
| 3 | Remove contaminants from specified area, if present. | This is necessary to avoid grease or oil causing contamination of tools and surface. NOTE Utilize appropriate personal protective equipment to protect from contact or injuries from solvents/detergents, dust, projectiles, and hand/power tools. |
| 4 | Remove existing coating or mill scale, rust, or weld slag, etc., to achieve specified profile. | Address hazardous coatings (e.g. containing asbestos or lead) in accordance with regulatory requirements and operator procedures. NOTE If coating to be applied meets existing coating the transition may be made by feathering the existing coating at the interface. |
| 5 | Ensure that surface preparation meets operator standards or specifications. | — |
| 6 | Make notifications per the operator’s procedures. | Follow the operator’s policies/procedures for appropriate documentation, notification protocol, and actions required. |